## Slide 1: RPC Production status for Engineering Module & Detector stack at IICHEP, Madurai
Shri. S.D.Kalmani
TIFR

## Slide 2
Part A
Manufacturing Process at Saint Gobain at Sriperumbudur,Chennai
RPC- “Glass Gap” – 400 number
  HV groove etching process
  Screen Printing : Surface resistance about 1 to 5 Mega Ohm
  Surface resistance measurements (plots)
  Gap Making : Semi automated process
  Leak Test
  QC certification and packing/transporting :IICHEP Madurai
  Storage at IICHEP

## Slide 3
Part B
Detector stack at IICHEP, Madurai
  Number of RPC of (1900 X 1800 )mm :12
  Leak Test
  Surface resistance measurements (plots)
  RPC Assembly
  Installation.
  Up gradation of electronic
  Results

## Slide 4
Engineering Module :
Detector size: 8 meters X 8 meters X 70 layers [RPC’s = 4 X 4 X 70L= 1120 and if 20 layers then 320 RPC’s]

## Slide 5
The “coated glass gap” with a gap of 2mm created in between two 3mm thick float glass with four gas nozzles, and these glasses are coated with conductive paint on the outer surface, while the surfaces inside the gap are cleaned and not coated. The 2mm gap is maintained by button spacers placed at distances of 200mm both along X and Y directions and by side spacers of thickness of 2mm, on the four edges. So a gap of 2mm is created inside the chamber and the buttons and side spacer are glued with 3M glue.
Schematic: Glass Gap

## Slide 6
Glass Cleaning and Drying Machine

## Slide 7: HV groove: Etching Process
HV groove for High voltage lug fixation is done by chemical etching process.
60% diluted Hydrofluoric acid has been used.
First HV groove Die will be fixed by checking TOP and Bottom glass selection using wax.
Near by surface covered with plastic paper to avoid damage due to HF acid.
Waited for 85 min.
Thrice replacing HF during this process.

## Slide 8
Wax
DIE
Etching process for HV Groove

## Slide 9
0.4mm Depth
Etched HV groove
HV Lug on the Painted glass

## Slide 10
Screen Printing
Stirrer cum Viscosity meter

## Slide 11
SCREEN PRINTING AND CURING
1. Screen printing has been done using Korean ink DC20 and DC1000 in proportion of 1:5.5.
2. IR drying temperature 110 degrees.
3. Surface resistance in range of 1M to 5 M ohm with 25 cm x 25 cm jig and with grid of 5 x 5 is acceptance criteria.

## Slide 12
Semi Automated RPC-Glass Gap Assembly machine
Button Selector Pot
Button Pickup
Glue Disp.
Button Pusher
Glue dispensing, button placing and side spacer glueing

## Slide 13
Leak Test: Developed by Suryanarayan
Sensor Board: Pressure and Temperature
Raspberry Pi board
Poster

## Slide 14
READY GLASS Gap
QC qualified Gap

## Slide 15
Preparation for Storage of Glass Gaps :IICHEP Madurai

## Slide 16: Detector stack at IICHEP, Madurai
Sample 14 gas gaps made at SG factory, Chennai for Testing and Qualifying at IICHEP Madurai.
Team of staff visited in batches for Installation and testing for about 3months .
M.Sc students actively participated

## Slide 17
Resistance and Pickup strip measurements

## Slide 21
Final RPC Detector

## Slide 22
Installation RPC

## Slide 25: Summary
Getting Industries into the R & D and then into production is almost done.
Presently 30 Glass gaps per month are being fabricated
Two INO member are station at Saint Gobain for day to day supervision and measurement work.
Noise free 12 layers of RPC detector in operation at IICHEP, Madurai
Up gradation of the existing electronics with newly tested RPC-DAQ will be implemented soon-
Next talk by Dr. B. Satyanarayana.

## Slide 26: Hope for early clearance from Tamilnadu Government to built the INO detector
Thank You