## Slide 1
Collaboration:
Helmut Zacharias, Benjamin Göhler, Matthias Kettner, Münster, Germany
Zeev Vager-Dep. of Particle Physics, WI
Sidney Cohen- Chemical Support, WI
Mudi Sheves and Noga Friedman-Organic Chemistry, WI
David Waldeck-Chemistry, University of Pittsburgh, USA
Yossi Paltiel, Hebrew University
Rafael Gutierrez and Giovanni Cuniberti, Dresden, Germany
Claudio Fontanesi and Luisa Schenetti, Modena, Italy
Sławomir Sęk, Jan Pawłowski, Joanna Juhaniewicz , Warsaw, Poland
The Chirality Induced Spin Selectivity (CISS) Effect-
From Spintronics to Electron Transfer in Biology
Dep. of Chemical Physics, Weizmann Institute, Rehovot, Israel

## Slide 2: How can we transfer electron efficiently in biology and in photovoltaic devices ?

## Slide 3
What is the “rifle effect”?
Coupling angular with linear momenta
How can it be transferred to molecular systems ?
Spin and chiral molecules
The rifle effect
Rifle is a gun with groves

## Slide 4: Electron Spin and Chirality How are they related?

## Slide 5: Zuoti Xie, Tal Markus, Sidney Cohen, Zeev Vager, Rafael Gutierrez, Nano Letters, 11, 4652–4655 (2011).
Spin dependent transport through double stranded DNA

## Slide 6
][][
Control

## Slide 7
][][
][][
Control

## Slide 8: α-helices Oligopeptides
][][
-Cys-(S-Acm)-(Ala-Leu)7-NH-(CH2)2-SH
Ala= alanine ; Leu= leucine
total length 2.8 nm
Vankayala Kiran and Sidney Cohen
ΔE= 0.5 eV

## Slide 9: Spintronics Devices
Spin valve based on the Giant Magneto Resistance effect
Problems: Low spin polarization at room temperature
Complex structure, hence expensive device.
Cannot be scaled down to below about 50 nm regime.

## Slide 10
CISS based spintronics
Shinto Mathew
 Helix oligopeptide

## Slide 11: L and D Cysteine/AlOx
In collaboration with the group of Yitzhak Mastai from Bar Ilan University
The Al2O3 is chiral

## Slide 12: Magnetic Memory-Spin Torque Transfer (STT)
Metal substrate
Chiral layer
Ferromagnet
Metal substrate
e-
The resistance increases with magnetization
Regular STT device
CISS based STT device

## Slide 13: Magnetic memory with no permanent magnet O. Ben Dor, S. Yochelis, S. P. Mathew, R. Naaman,Y.Paltiel, Nat. Comm.4, 2256 (2013).

## Slide 14
Spin Dependent Electrochemistry
Prof. Claudio Fontanesi, Dr. Debabrata Mishra, Dr. Prakash Mondal, Dr. Hila Einati

## Slide 15: CV curves of the 1mM K4[Fe(CN)6]/ K3[Fe(CN)6] redox couple in a pH = 7 (TRIS) buffered, (a) CV for Ni bare surface as working electrode (b) CV obtained using the bR thin film physisorbed on Ni working electrode; arrows in the figures indicate the two possible directions (conventionally UP and DOWN) of the magnetic field (H = 0.35 T); which is orthogonal to the surface of the working electrode. The inset in Fig.1 (b) shows CVs of a bR/Ni thin film at H = 0: (i) freshly deposited bR on Ni and (ii) after the “electrochemical burning” of the bR.
Bacteriorhodopsin-Spin dependent electrochemistry

## Slide 16: Conduction through -helices oligopeptides Studied by electrochemistry
6.5% polarization/nm
In DNA: 2.7% polarization/nm
Molecules synthesized by Sławomir Sęk, Jan Pawłowski, Joanna Juhaniewicz, Warsaw, Poland
-Cys-(S-Acm)-(Ala-Leu)7-NH-(CH2)2-SH
Ala= alanine ; Leu= leucine

## Slide 17: CV plot for PCT-L coated Ni electrode when the redox couple is achiral ferrocene.
PCT-L coated gold electrode,
when electrons are not spin polarized
poly{methyl (2R)-3-(2,2'-bithiophen-4-ylsulfanyl)-2-[(tert-butoxycarbonyl)amino]propanoate} (PCT-L)
Chiral Conductive Polymer

## Slide 19: How the Chiral Induced Spin Selectivity (CISS) effect can be rationalized ?
Typically spin filtering is observed either in ferromagnetic materials or in materials with very high spin-orbit coupling.

## Slide 20: The Mechanism
Electron is passing through helical-shape
potential.
Because of the lack of inversion symmetry, in the rest frame of the passing electron there is a magnetic field that acts on the spin.
The angular distribution of the electrons scattered from the potential depends on the electrons’ spin (like in Mott polarimeter).
The electrical field acting on the electron must confine it to the radius of the molecule.
The sign of the spin state stabilized depends the sign of the velocity (v) and of the electric field.
The sign of the electric field depends on the chirality and on the field across the molecule – either the applied field or the dipole moment.

## Slide 24
Beff=
Beff=
/2
Me=9x10-31kg;
v(for 1 eV)=6x105 m/sec
R=0.5 nm=0.5x10-9m
Hence
Beff =6750 Tesla
The spin orbit coupling is given by:
The splitting between the states
corresponds to 2=390 meV
Effective Hamiltonian

## Slide 25: Avoided Elastic Back Scattering Based on concepts developed for Quantum Hall and Topological Insulators.
Since Y(0)=-Y(2p)
The two paths destructively interfere

## Slide 26
Photo-Spintronics Device
C
Ni(200nm)/Al2O3(0.5nm)/Ag(50nm)
K. S. Kumar, N. Kantor-Uriel, S. P. Mathew, R. Guliamov, R. Naaman, Device for Measuring Spin Selectivity in Electron Transfer, Phys. Chem. Chem. Phys., 2013, 15, 18357-18362 (2013).
K. Senthil Kumar and R. Naaman, Langmuir, 28, 14514-14517 (2012) .

## Slide 27: Capacitive Device
e
ΔV=V

## Slide 28: Capacitive Device
e
ΔV=V

## Slide 29
Silver thickness and temperature dependent
The value of the P at low temperature (about 20%) is similar to that observed in former CISS studies at room temperature.
The temperature dependence indicates spin-phonons interactions.
Spin polarization P = (V↑-V↓)/V↑↓
50 nm Ag
35 nm Ag

## Slide 30
DNA length dependent measurement at 290K
The spin polarization increases with the length of the DNA, as obtained before for photoelectrons transmitted through DNA.

## Slide 31: Spin Effect in Electron Transfer in Photosystem 1
In collaboration with Itai Carmeli and Chanoch Carmeli, Tel Aviv University
Itai Carmeli, Karuppannan Senthil Kumar, Omri Hieflero, Chanoch Carmeli, Ron Naaman, Angew. Chemie 53, 8953 –8958 (2014).

## Slide 32
Spin polarization was observed in the first stage of the electron transfer using Electron Paramagnetic Resonance (EPR)

## Slide 33
V
Ni
AlOx
Ag
h
e-
V
Ni
AlOx
Ag
h
e-
Light on
Light off
Light on
Light off
Work function decreases
Work function increases

## Slide 35
The spin effect in electron transfer in Photosystem I
The spin selectivity in electron transfer through photosystem one is
80±20%.
The observations are consistent with the EPR studies.
The spin selectivity can be related to the high electron transfer yield.

## Slide 36: Oxidation of water- In photosynthesis and for producing hydrogen as a fuel
2OH- O2+H2
2H+ H2
-2e-
+2e-
Problems with the artificial process:
High over-potential of 0.6 V makes the hydrogen production inefficient.
Non selective oxidation

## Slide 37: Where is the problem?
Our suggestion- In the spin.
O inside OH- has the following electronic configuration:
2S
2P

## Slide 38: Now one electron is removed from each OH- and each oxygen atom is supposed to be left in its triplet ground electronic states
2S
2P
If different spins are transferred
The system is left in a singlet potential energy surface and within the
ground singlet state of the oxygen cannot be formed.
If the same spins are transferred than the two oxygen atoms are on high spin surface
and the ground state can be formed.
2S
2P

## Slide 39: Our experimental setup
Dr. Wilbert Mtangi
Dr. Kiran Vankayala
Prof. Claudio Fontanesi

## Slide 40: The photocurrent density as a function of the potential vs. Ag/AgCl electrode
MPA- C3 alkyl chain
MUA-C11 alkyl chain
Oligo- 10 amino acids long
-helix oligopeptide
C3
C11
Oligo

## Slide 41: Hydrogen production as a function of time

## Slide 42: Spin alignment controlled water oxidation
The origin of the large over-potential and the non-specificity is the requirement that the two oxygen atoms will be in close proximity, so that exchange interaction will induce the spin alignment.
By having spin alignment controlled, the need for proximity is removed and reaction takes place at larger cross-section. Therefore, no high over-potential is required and higher selectivity is obtained.
The chiral-controlled effect brings the artificial water oxidation system closer to the natural one.

## Slide 43: Summary
The CISS effect introduces chiral molecules as a new spintronics material.
It may explain long range electron transfer processes in Biology as well as multiple electrons reactions, and effects of weak magnetic fields in Biology.
It allows to develop spintronics devices with no permanent ferromagnets.
Because the effect is temperature and size independent it removes many of the constrains in spintronics.
It may open new opportunities in producing materials via multiple electrons reactions.

## Slide 44
Itai Carmeli, Supratim Gua Ray, Tal Markus, Zuoti Xie, Gilad Gotesman,
Sivan Kober, Senthil Karuppannan, Meital Eckshtain*, Nirit Kantor*, Debabrata Mishra*, Shinto Mathew*, Prakash Mondal*, Partha Roy*, Eyal Capua*, Shirley Daube, Hila Einati*, Rahamim Guliamov*,

## Slide 45: Thank You
Volkswagen Stiftung